## Slide 1: Electrowinning Process for Copper
Group 2
Solomon Ahedor 1981322
Christian Mills 1983822
Kingsley Sarpong 1985722
Christian Oduro 7279521
Bettina Shika Gemegah 1983122
Lordina Erskine 1982922
Rashid Abdul Sumaila 1985822
Emmanuel Kyei Sarfo 1985522
Kelvin Nana Adjei 7278821
Supervisor: Ing. Henry Agbe

## Slide 2: Content
Introduction
Electrochemical Principles
Electrowinning vs. Electrorefining
Electrowinning Cell Design
Overall Process Flow
Typical Operating Parameters
Operating Challenges & Advances
Cathode Harvesting & Quality
Industrial Plant Case Studies
Recent Advances & Future Outlook
Environmental & Economic Significance
Conclusion
References

## Slide 3: Introduction
Copper electrowinning (EW) recovers metallic copper from a purified sulfate solution by passing a DC current between an insoluble anode and a cathode.
Final step of the hydrometallurgical route (SX-EW), treating oxide and low-grade ores.
SX-EW accounts for approximately 20% of global copper production.
Operates in a complementary role to conventional smelter-refineries.

## Slide 4: Electrochemical Principles
• Cathode Reaction: Cu²⁺ + 2e⁻ → Cu⁰ (E° = +0.34 V)
• Anode Reaction: H₂O → ½O₂ + 2H⁺ + 2e⁻ (E° = -1.23 V)
• The overall cell reaction is thermodynamically unfavourable, requiring applied voltage.
• Mass deposited is governed by Faraday's laws of electrolysis.
• Current efficiency is typically 88–95% due to parasitic reactions (e.g., ferric ion reduction).

## Slide 5: Electrowinning vs. Electrorefining
• Electrorefining (ER): Uses impure copper anodes (dissolution). Voltage ~0.2–0.3V. Specific energy ~200–300 kWh/t Cu. Produces ~95% of world copper.
• Electrowinning (EW): Uses inert lead alloy or coated titanium anodes (oxygen evolution). Voltage ~2.0–2.2V. Specific energy ~1,800–2,000 kWh/t Cu. Produces ~20% of world copper (via SX-EW).
• EW is indispensable for recovering copper directly from dissolved leach solutions without smelting.

## Slide 6: Electrowinning Cell Design
• Tanks are typically polymer concrete, electrically isolated.
• Alternating flat rectangular anodes and cathodes are suspended vertically.
• Anodes: Lead-calcium-tin/antimony alloys or dimensionally stable coated titanium.
• Cathodes: Historically copper starter sheets; modern plants use permanent stainless-steel blanks.
• Cobalt sulfate (100–200 mg/L) suppresses anode corrosion. Guar gum promotes smooth deposits.

## Slide 7: Overall Process Flow (Ore to Cathode)
1. Leaching: Oxide ores irrigated with dilute H₂SO₄ to produce a pregnant leach solution (PLS).
2. Solvent Extraction (SX): Organic extractant selectively binds copper, leaving impurities in raffinate. Copper is then stripped into a pure, concentrated advance electrolyte.
3. Electrowinning (EW): Advance electrolyte is fed to the tankhouse. Copper deposits on cathodes; spent electrolyte returns to SX.

## Slide 8: Typical Operating Parameters
• Cu²⁺ concentration: 35–45 g/L
• H₂SO₄ concentration: 150–180 g/L
• Electrolyte temperature: 40–50 °C
• Current density: 160–370 A/m² (up to >450 A/m² in modern plants)
• Cell voltage: 2.0–2.2 V per cell
• Current efficiency: 88–95%
• Specific energy consumption: 1,800–2,000 kWh/t Cu
• Deposition cycle: 5–9 days

## Slide 9: Operating Challenges & Advances
• Iron Impurities: Fe³⁺ migration causes parasitic current-efficiency loss.
• Acid Mist: Oxygen bubbles entrain corrosive electrolyte. Controlled using floating balls, mats, or chemical suppressants (e.g., fluorochemicals, glycyrrhizin).
• Advances: Permanent stainless-steel cathodes, robotic stripping machines, and alternative anode reactions (ferrous/ferric or sulfur-dioxide-depolarised) to lower cell voltage.

## Slide 10: Cathode Harvesting and Product Quality
Deposition Cycle: Harvested after 5 to 9 days (6-12 mm thick, 40-60 kg per sheet)
Stripping: Mechanical stripping machines peel copper from permanent stainless steel blanks
Washing: Hot water wash (70-80°C) to remove residual acid and sulfate salts
Quality: LME Grade A purity (>99.99% Cu)
Impurity Limits: S ≤ 5 ppm, Pb ≤ 2 ppm, Fe ≤ 2 ppm

## Slide 11: Industrial Plant Case Studies
Cerro Verde, Peru:
  - Latin America's first commercial SX-EW plant
  - Expanded capacity to 48,000 tonnes/year at 250 A/m²
  - Optimized to 368 A/m², doubling throughput while maintaining Grade A quality
KCM Tankhouse, Zambia:
  - Key controls: acid tenor, organic entrainment, cobalt sulfate and thiourea dosing
  - Achieves 92% current efficiency with automated desludging

## Slide 12: Recent Advances and Future Outlook
Low-Voltage Anode Reactions: Ferrous/ferric or SO2-depolarized anodes can lower voltage below 1.5 V, yielding 30-40% energy savings
MMO DSA Anodes: Catalytic coatings on titanium lower overpotential and eliminate lead sludge
Robotics & Automation: Robotic crane harvesting, AI-driven dosing, and automated short-circuit laser scanning
Ultra-High Current Density: Optimized fluid dynamics enable operation at >450 A/m²

## Slide 13: Environmental and Economic Significance
Sustainable Pathway: Zero direct greenhouse gas emissions during the electrolysis process
Resource Efficiency: Enables economic processing of low-grade oxide ores and e-waste
Energy Consumption: Highly energy intensive (1,800 to 2,000 kWh/tonne Cu)
Future Shift: Industry is transitioning towards renewable sources (solar/hydro) to lower indirect carbon footprint

## Slide 14: Conclusion
Electrowinning remains a vital process for converting copper leach solutions into high-purity cathode metal
Modern plants achieve >94% current efficiency by integrating permanent stainless steel cathodes and optimized additives
The technology is continuously advancing towards lower-overpotential anodes and fully automated tankhouse operations

## Slide 15: References
Bartos, P.J. (2002) 'SX-EW copper and the technology cycle', Resources Policy, 28(3–4).
Davenport, W.G. et al. (2002) Extractive Metallurgy of Copper. 4th edn.
Schlesinger, M.E. et al. (2011) Extractive Metallurgy of Copper. 5th edn.
SAIMM (2002) 'Copper recovery using leach/solvent extraction/electrowinning technology'.

## Slide 16: THANK YOU